PRODUCT DATA SHEET

POWDER NBR P1850

PRODUCT DESCRIPTION:

P1850 	is processed through special technics after butadiene and acrylonitrile are copolymerized under low temperature.

P1850 	is powder form macromolecule rubber.

P1850  	is environmental friendly material. It has passed various measures for SGS Test and does not contain 16P.

PRODUCT CHARACTERISTICS:

- Controls plasticizer from precipitation – can absorb low molecular plasticizers after addition, thereby to reduce or avoid low molecular plasticizers from precipitation

- Environmental friendly － will not cause environmental pollution

- Not harmful to human body – P1850 is suitable to use in food and human body contact PVC products industries.

PROPERTIES OF APPLICATIONS：

P1850 can provide the following properties to PVC products:

- Heat and low temperature resistance properties

- Oil resistance property

- Increases elongation at break

- Improves compressive deformation properties

- Improves product’s rebound resilience

- Low temperature flexibility

APPLICATIONS:

P1850 can be used in thermoplastic elastomer materials to fully or partially replace of liquid plasticizer.

| - PVC Cables and Wires | - Friction materials etc. |
| --- | --- |
| - Auto-mobile & construction use sealant, refrigerator sealant | - Plumbing pipe gasket seal |
| - Auto-mobile fuel pipe, hosepipe | - Auto mobile dust cover, Mine-use protective cover |
| - Rubber Conveyer belt, V-belt | - Thin film, leatheroid, banner |
| - Shoe products (Galoshes and Safety boots) |  |

TECHNICAL DATA:

| Polymer Name | P1850 |
| --- | --- |
| Method of polymerization | Low temperature polymerization |
| Acrylonitrile content ( % ) | 20 |
| Mooney Viscosity ML1+4 @100℃ | 50 |
| Parting agent | Chemicals |
| Particle size (mesh) | 40 |
| Degree of crosslinking | Linear |
| Specific Gravity | 0.98 |
| Stabilizer | Non-pollution |
| Emulsifier | Aliphatic acid |
| Appearance | Powder form |
| Packaging | 25KG |
| Application and Properties | PVC products |